## Slide 1
Vasilyev Yury Emmanuilovich Ph.D., associate professor, Executive Director of MADI innovative infrastructure development program
vas@madi-dt.ru
Evgenyeva Anna Glebovna, Ph.D. student
Moscow State Automobile & Road Technical University
Technopark MADI in the process of an innovation sphere formation in Russian Automobile & Road complex
Prague 2012

## Slide 2: Federal law №127-FZ, dated 02.08.2009
«MADI»
SIE «MADI – Road Technologies»
SIE "Monitoring of highways and road technologies"
SIE "MADI – Integrated Intelligent Transport Systems"
SIE "Technopark MADI"
SIE "Ultrateh"

## Slide 3
Modified bitumen
Polymers
Crumb rubber
«BITREK»
«UNIREM»
Sulphur
Construction bitumen

## Slide 4
Asphalt concrete
high-density
dense
pure bitumen binder
with modifier «UNIREM»
SMA
mastic
polymer-modified binder
rubber-bitumen binder «BITREK»
sulfur-bitumen binder

## Slide 5
Chart: PLASTIC RUTTING
| 0 | 2000 | 4000 | 6000 | 8000 | 10000 | 12000 | 14000 | 16000 | 18000 | 20000 | 22000 | 24000 | 26000
БНД 60/90 | 0 | 1.3 | 1.7 | 2 | 2.4 | 2.7 | 2.8 | 3 | 3.2 | 3.5 | 3.7 | 4 | 4.3 | 4.5
БИТРЭК | 0 | 1 | 1.2 | 1.4 | 1.5 | 1.6 | 1.7 | 1.8 | 1.8 | 1.9 | 2 | 2 | 2 | 2.1
ПБВ 60 | 0 | 0.6 | 0.7 | 0.8 | 0.8 | 0.9 | 1 | 1 | 1.1 | 1.2 | 1.2 | 1.3 | 1.4 | 1.5
СБВ | 0 | 0.6 | 0.6 | 0.7 | 0.8 | 0.9 | 0.9 | 0.9 | 1 | 1 | 1.1 | 1.2 | 1.3 | 1.4
Chart: ABRASIVE WEAR RUTTING
| 0 | 2500 | 5000 | 7500 | 10000 | 12500 | 15000 | 17500 | 20000 | 22500 | 25000 | 27500 | 30000 | 32500
БНД 60/90 | 0 | 1.2 | 1.4 | 1.5 | 1.7 | 1.8 | 1.8 | 1.9 | 2 | 2 | 2.1 | 2.2 | 2.3 | 2.4
БИТРЭК | 0 | 1 | 1.2 | 1.4 | 1.5 | 1.6 | 1.7 | 1.8 | 1.8 | 1.9 | 2 | 2 | 2 | 2.1
ПБВ 60 | 0 | 0.8 | 1.1 | 1.2 | 1.3 | 1.4 | 1.5 | 1.7 | 1.7 | 1.7 | 1.8 | 1.8 | 1.9 | 1.9
СБВ | 0 | 0.6 | 0.6 | 0.7 | 0.8 | 0.9 | 0.9 | 0.9 | 1 | 1 | 1.1 | 1.2 | 1.3 | 1.4
BND 60/90
BITREK
PMB 60
SBB

## Slide 6
wear-resistance
rutting resistance
cracking resistance
noisiness
thermal resistance
…

## Slide 7: MAIN CHARACTERISTICS OF «ADS-MADI»
12 м
1,5 м
Продольная ровность
Transverse evenness
Scanning of surface
High frequency georadar
Longitudinal evenness
Low frequency georadar

## Slide 9: LAYOUT OF EQUIPMENT ON THE MOBILE LABORATORY «ADS-MADI»
Low frequency georadar,
diapason 7 – 10 m
Acceleration sensor of the longitudinal evenness measurement system
Laser sensor of the longitudinal evenness measurement system
High frequency georadar, diapason up to
100 cm
Lamp of the line camera of the road surface
Line camera of side looking
Line camera of the road surface
Camera of the volumetric scanner
Laser generator of the volumetric scanner line
BASIC SYSTEMS
Longitudinal evenness fixation system - 1d
Object detection fixation system (defects, horizontal road marking, etc.) – 2d
Transverse evenness gaging system – 3d
Georadar sounding system – 4d
Position control system

## Slide 10
MOSCOW RING ROAD
5th lane
2d
lane
1st lane
3d
lane
4th lane
Value, mm
Value, mm
Value, mm

## Slide 11
LABORATORY RUTTING TESTS
b)
c)

## Slide 12
France
Slovak Republic
Ukrain

## Slide 13
UNIVERSAL TEST FACILITIES COMPLEX
PAVEMENT AND TYRES TESTING
Phase I (light stand)
– December 2011
Phase II (heavy stand)
– November 2012

## Slide 14
Parameters | Stand | 
 | «light» | «heavy»
Diameter, m | 30 ± 2 | 30 ± 2
Speed, km per hour | up to140 | up to 80
Mass, kg | up to 600 | up to 7 000
Lane width, m | 3,75 | 3,75

## Slide 15
Stud influence
Traction and driven wheels
Comparison tests for 3 different material types (А, В, С)
Speed rate, up to 140 km per hour
Speed-up and slowdown
V = 140 km per hour

## Slide 16
Thank you for your attention!
Any questions?
vas@madi-dt.ru